**DIVISION 09 – FINISHES**

**SECTION 09 65 13 – 13 RESILIENT WALL BASE**

*This document is provided to assist in the preparation of a Project or Master Specification and has been formatted in accordance with the Construction Specifications Institute (CSI)’s MasterFormat®. Ensure the latest publicized version of all product information for this specification, Roppe will not be liable for any damages arising out of the use of any information or specifications found in this documents.*

BEGINNING OF SECTION 09 65 13 – 13

**PART 1 – GENERAL**

1. **GENERAL PROVISIONS**
   1. Drawings and general provisions of the Contract, including General and Supplementary Conditions of Division 01 General Requirements, Specification Sections, apply to this section.
2. **SUMMARY**
   1. Section includes:
      1. Resilient Wall Base
3. S**UBMITTALS, RELATED DOCUMENTS**
   1. **General:** Submit listed submittals in accordance with Conditions of the Contract and Division 1 Submittal Procedures.
   2. **Product Data:** Submit manufacturers documentation for each material and accessory proposed for use (available at [www.roppe.com](http://www.roppe.com)).
      1. Technical data sheet
      2. Care & maintenance document
      3. Warranty
   3. **LEED Submittals:**
      1. Product Data for Credit EQ 4.1: For adhesives, including printed statement of VOC content and chemical components.
   4. **Samples for Initial Selection**: For each type of product indicated.
   5. **Samples for Verification**: For each type of product indicated, in manufacturer’s standard- size samples of each resilient product color, texture and pattern required.
   6. **Product Schedule**: For resilient products. Use same designations indicated on Drawings.
4. **QUALITY ASSURANCE**
   1. Manufacturer Qualifications: Provide resilient wall base materials manufactured in the United States of America by a firm with a minimum of 10 years’ experience with resilient vinyl materials of type equivalent to those specified.
   2. Provide resilient wall base, flooring materials, adhesives, accessories and subfloor preparation products from one manufacturer to ensure color matching and compatibility.
   3. Manufacturer shall be capable of providing technical training and technical field service representation.
5. **RELATED WORK**
   1. Installer must be professional, licensed, insured and acceptable to manufacturer of resilient flooring materials. Project Managers or Field Supervisors must be INSTALL (International Standards & Training Alliance) certified CFI (Certified Floorcovering Installers) Certified and/or an FCICA (The Flooring Contractors Association) CIM (Certified Installation Manager) for the requirements of the project or equivalent.
6. **DELIVERY, STORAGE AND HANDLING**
   1. Store resilient products and installation materials in dry spaces protected from the weather, with ambient temperatures maintained within the range recommended by Roppe of 65 degrees F (18degrees C) and 85 degrees F (29 degrees C).
7. **PROJECT CONDITIONS**
   1. Install resilient product s after other finishing operations, including painting, have been completed.
   2. Maintain ambient temperatures within range of (± 10 degrees F) 65 degrees (18 degrees C) and 85 degrees F (29 degrees C) in the spaces to receive the resilient products during:
      1. 48 hours before installation.
      2. During installation.
      3. 48 hours after installation.
   3. Maintain relative humidity between 40% and 65% during installation.
   4. Avoid conditions in which dew point causes condensation on the installation surface.
8. **WARRANTY**
   1. Provide manufacturer’s standard limited commercial warranty to cover manufacturing defects

**PART 2 - PRODUCTS**

*Note To specifier: remove and amend sections as necessary.*

1. **MANUFACTURER**
   1. Basis-of-Design: Roppe Corporation | 1602 N Union St. | Fostoria, OH 44830 | P: (800) 537-9527
   2. Substitutions: No substitutions permitted
2. **PRODUCTS**
   1. ROPPE THERMOPLASTIC VINYL (TV) WALL BASE specify - specify vinyl wall base with the following characteristics: **Meets the performance requirements for the following Industry Standards:**
      1. ASTM F1861, Standard Specification for Resilient Wall Base, Type TV (vinyl, thermoplastic), Group 2 (solid, layered), Style A&B (Straight, Cove)
      2. ASTM E84, Standard Test Method for Surface Burning Characteristics of Building Materials, Class A
      3. ASTM E648 (NFPA 253), Standard Test Method for Critical Radiant Flux, Class 1, >0.45 W/cm²
      4. ASTM E662 (NFPA 258), Standard Test Method for Smoke Density, Passes, <450
      5. ASTM F137, Standard Test Method for Flexibility of Resilient Flooring Materials protocols, Passes
      6. ASTM F386, Standard Test Method for Thickness of Resilient Flooring Materials Having Flat Surfaces, Passes
      7. ASTM F925, Standard Test Method for Resistance to Chemicals of Resilient Flooring, Excellent
      8. ASTM F1515, Standard Test Method for Measuring Light Stability of Resilient Flooring protocols, Passes
      9. NFPA 253, Test Method for Critical Radiant Flux of Floor Covering Systems Using a Radiant Energy Source
      10. NFPA 255, Standard Method of Test of Surface Burning Characteristics of Building Materials
      11. NFPA 258, Test Method for Specific Density of Smoke Generated by Solid Materials
      12. Specify size by name and description: *(remove all but the size selecting)*  [Roppe 2 1/2″ Vinyl Cove Base,](https://roppe.com/wp-content/uploads/2017/07/Roppe2.5InchVinylCoveBaseProductSubmittal.pdf) [Roppe 2 1/2″ Vinyl No Toe Base,](https://roppe.com/wp-content/uploads/2017/07/Roppe2.5InchVinylNoToeBaseProductSubmittal.pdf) [Roppe 4″ Vinyl Cove Base,](https://roppe.com/wp-content/uploads/2017/07/Roppe4InchVinylCoveBaseProductSubmittal.pdf) [Roppe 4″ Vinyl No Toe Base,](https://roppe.com/wp-content/uploads/2017/07/Roppe4InchVinylNoToeBaseProductSubmittal.pdf) [Roppe 6″ Vinyl Cove Base,](https://roppe.com/wp-content/uploads/2017/07/Roppe6InchVinylCoveBaseProductSubmittal.pdf) [Roppe 6″ Vinyl No Toe Base](https://roppe.com/wp-content/uploads/2017/07/Roppe6InchVinylNoToeBaseProductSubmittal.pdf)
      13. Specify style by Alpha and name *(remove all but the style selecting)* A. Straight or B. Cove
      14. Specify Color by Number and Name: *(remove all but the color selecting)* 100 black, 177 steel blue, 150 dark gray, 193 black brown, 123 charcoal, 114 lunar dust, 129 dolphin, 178 pewter, 194 burnt umber, 148 steel gray, 175 slate, 174 smoke, 197 iceberg, 110 brown, 147 light brown, 182 toffee, 623 nutmeg, 624 chameleon, 140 fawn, 191 camel, 125 fig, 171 sandstone, 130 buckskin, 198 ivory, 632 flax, 184 almond, 170 white, 131 bisque, 127 harvest yellow, 631 sahara, 639 beigewood, 640 creekbed 122 natural,, 195 light gray, 663 aged fern, 648 pear green, 647 spring dill, 646 gecko, 160 forest green, 649 sweet basil, 169 hunter green, 662 envy, 118 peacock, 187 blue, 139 deep navy, 627 mariner, 618 aubergine, 665 horizon, 664 blue jay, 656 bluebell, 654 lagoon, 638 cadet, 637 night mist, 655 peaceful blue, 657 sorbet, 658 berry ice, 6211 merlin, 659 grape, 186 red, 137 cinnabar, 188 brick, 617 terracotta, 660 citrus, 661 marmalade, 643 mimosa, 644 sunbeam, 642 jonquil, 645 blonde, 641 moonrise, 161 snow
      15. TV WALL BASE vinyl wall base is SCS FloorScore® Certified and meets California Specifications Section 01350
      16. TV WALL BASE vinyl wall base is 100% recyclable
      17. TV WALL BASE vinyl wall base and accessories do not contain chemicals that may be hazardous to human health
      18. TV WALL BASE vinyl wall base meets NSF 332 Gold Criteria
      19. TV WALL BASE vinyl wall base meets CHPS Criteria
      20. TV WALL BASE vinyl wall base is manufactured in the U.S.A.
      21. TV WALL BASE vinyl wall base is free of materials known to be teratogenic, mutagenic or carcinogenic
      22. TV WALL BASE vinyl wall base is free of Halogens
      23. TV WALL BASE vinyl wall base is free of Asbestos
      24. TV WALL BASE vinyl wall base is free of Phthalates
      25. TV WALL BASE vinyl wall base is free of Heavy Metals
3. **INSTALLATION AND MAINTENANCE MATERIALS**
   1. Substrate/Background Preparation Products:
      1. Adhesives: Adhesives should be selected based on the site conditions and use of the space being installed
   2. Recommended Adhesive Products:
      1. Excelsior WB-600 Acrylic Wall Base Adhesive by Roppe
         1. Unit Size: 30 oz. cartridge, 1 Gallon & 4 Gallon
         2. Coverage: 30 – 70 linear feet per cartridge, 180 – 340 linear feet per gallon
         3. Standard installations over porous backgrounds
         4. 100 % solids, solvent free and low VOCs
         5. Hard set adhesive adding to dimensionally stable materials
         6. Excellent sheer strength
      2. Excelsior C-630 Contact Adhesive provided by Roppe
         1. Unit Size: 1 Quart
         2. Coverage: 20 – 40 Square Feet per unit / 120 – 140 Linear Feet per unit
         3. Standard installations over porous and non-porous substrates
         4. Hard set adhesive adding to dimensionally stable materials
         5. Excellent sheer strength
         6. Superior bond strength
         7. Great for environments with topical moisture
   3. **Accessories:** Items needed to complete the installation. Recommended accessory products:
      1. Inside corners
      2. Outside corners
      3. Color-matched caulks
   4. **Maintenance Materials:** Proper maintenance of the installation is critical to the long term performance of the flooring products being specified. Using the appropriate chemicals to maintain the product according to the environment in which it is specified is critical. Recommend maintenance products:
      1. Excelsior NC-900, All-Purpose Neutral pH Cleaner provided by Roppe
         1. For initial maintenance
         2. For daily and routine maintenance
      2. Excelsior FR-920 Finish Remover
         1. For removing of topically applied finishes.
         2. Highly concentrated, cuts through multiple layers of floor finish.

**PART 3 – EXECUTION**

1. **GENERAL**
   1. **General Contractor Responsibilities:**
      1. Supply a safe, climate controlled building as detailed in Roppe Technical Data Sheets.
      2. Ensure substrate/background meets the requirements of ASTM F1861, Roppe Technical Data Sheets and Excelsior Technical Data Sheets.
      3. Provide a secure storage area that is maintained permanently or temporarily at normal operating temperature and humidity conditions between 65° F and 85° F and between 40% and 65% relative humidity, for at least 48-hours prior to and during the application of the wall base, so the contractor can acclimate the vinyl base materials per manufacturer’s instructions.
      4. Provide an installation area that is weather tight and maintained either permanently or temporarily at ambient service temperature and humidity. Normal operating temperature and humidity conditions are between 65° F and 85° F and between 40% and 65% relative humidity, for at least 48-hours prior to and during the application of the wall base per the manufacturer’s instructions.
      5. Ensure areas with direct prolonged exposure to sunlight are protected with protective UVA/UVB restrictive coatings or films.
      6. In areas where the walls are subject to direct sunlight through doors or windows, the doors and windows should be covered using blinds, curtains, cardboard or similar for the time of the installation and 72-hours after the installation to allow the adhesive to cure. Note: These areas should be installed using wet adhesives only.
      7. Conduct initial maintenance prior to final usage per the Roppe Care & Maintenance Documents. Do not conduct initial maintenance until adhesive has cured per the adhesive technical data.
      8. Provide trained installers that are professional, licensed, insured and acceptable to manufacturer of resilient vinyl wall base materials.
      9. Ensure installers or installation teams meet one of the following requirements:
         1. Have completed INSTALL (International Standards & Training Alliance)
         2. CFI (Certified Floorcovering Installers) training programs
         3. Certified by INSTALL or CFI.
         4. Are being supervised by Project Managers or Field Supervisors that are INSTALL (International Standards & Training Alliance) certified, CFI (Certified Floorcovering Installers) Certified and/or an FCICA (The Flooring Contractors Association) CIM (Certified Installation Manager).
      10. Follow all requirements in the appropriate Roppe and/or Excelsior Technical Data Sheets, Care & Maintenance Documents, Warranties and other technical documents or instructions.
2. **EXAMINATION**
   1. **General**: Follow guidelines laid out in Division 01, Section 01 71 00 – Examination and Preparation, as well as Section 01 43 00 – Quality Assurance.
   2. **Verification of Conditions:** Inspect all substrates/backgrounds to ensure they are clean, smooth, permanently dry, structurally sound and without voids. Confirm all areas are properly sealed and acclimated per manufacturer’s requirements.
   3. **Verification of Products:** In accordance with manufacturer’s installation requirements, visually inspect material for size, style, color or visual defects prior to installing. Any material that is incorrect or visually defective shall not be installed.
3. **SUBSTRATE/BACKGROUND PREPARATION**
   1. **General**: Follow guidelines laid out in Division 01, Section 01 71 00 – Examination and preparation. All work required ensuring substrate/background meets manufacturers’ guidelines are the responsibility of the general contractor.
   2. **Preparation**: Ensure substrate/background meets the requirements of ASTM F1861 for resilient wall base and/or Roppe Technical Data Sheets and Excelsior Technical Data Sheets.
      1. Substrates/backgrounds must be free of visible water or moisture, dust, sealers, paint, residual adhesives and adhesive removers, solvents, wax, oil, grease, mold, mildew and any other extraneous coating, film, material or foreign matter.
      2. Acclimate all products to be used during the installation and the installation environment prior to installation according to the manufacturers written instructions.
      3. Fill cracks, holes, depressions and irregularities in the substrate/background to prevent transferring through to the surface of the resilient wall base.
4. INSTALLATION
   1. **General**: Follow all relevant guidelines detailed in Division 01, as well as wall base and adhesive manufacturer’s technical data sheets.
   2. **Resilient Vinyl Wall Base:** Install material in accordance with manufacturer’s recommendations.
      1. Select the appropriate adhesive for the application and job site conditions.
      2. Install material according to roll sequence or with like run numbers.
      3. Ensure material is rolled appropriately into the adhesive using a hand roller.
5. **CLEANING & MAINTENANCE**
   1. **General**: Clean up installation area and vacuum dust or wipe material to remove any dirt, dust or debris.
   2. **Initial Maintenance**: Conduct initial maintenance per the manufacturer’s recommended procedures stated in the Maintenance Documents. All documentation is available upon request or from the Roppe website. Excelsior Cleaning products are the recommended products for use. All can be found linked to the product on the Roppe website or at [www.excelsiorproducts.net](http://www.excelsiorproducts.net).
   3. **Regular Maintenance**: Conduct maintenance on regular intervals as needed. Insufficient cleaning will reduce the wear life of the wall base and alter the aesthetic properties of the wall base. The amount of maintenance depends directly upon the amount of dirt and particulates the area is subjected to.
6. **CLOSEOUT ACTIVITIES**
   1. **General**: Follow all federal, state and local requirements and Division 01 Section 01 76 00 – Protecting Installed Construction and Section 01 78 00 – Closeout Submittal requirements for these activities, protecting installed construction.
   2. **Protection**: Protect newly installed material from damage by other trades. Be sure all construction debris is picked up and vacuumed or removed prior to leaving the area. Limit usage and foot traffic according to the adhesive's requirements. When moving appliances or heavy furniture, protect wall base from scuffing and tearing using temporary floor protection as well.

END OF SECTION 09 65 13 - 13